Whispering gallery modes in indium oxide hexagonal microcavities

Hongxing Dong,1 Zhanghai Chen,1,a_ Liaoxin Sun,1 Jian Lu,1 Wei Xie,1 H. Hoe Tan,2Chennupati Jagadish,2 and Xuechu Shen1

1Department of Physics, Surface Physics Laboratory, Advanced Materials Laboratory, Fudan University,Shanghai 200433, China

2Department of Electronic Materials Engineering, Research School of Physics and Engineering,

The Australian National University, Canberra, Australian Capital Territory 0200, Australia

We report on the use of In2O3 nanowires with hexagonal cross section as optical whispering gallery resonators. The single-crystal In2O3 nanowires were fabricated by an in situ thermal oxidation method. Whispering gallery modes (WGMs) in the visible spectral range were directly observed at room temperature. Due to the slight tapering of the nanowires, the energies and orders of the WGMs were modulated when excitations were scanned along the c-axis (length) of the nanowires. The experimental results were explained and fitted well with a plane wave interference model and Cauchy dispersion formula for refractive indices.