Unusual band-gap and band-edge bowing of SnxGe1-x alloys

Wan-Jian Yin and Xin-Gao Gong

Department of Physics, Fudan University, Shanghai, China

Su-Huai Wei

National Renewable Energy Laboratory, Golden, Colarado, USA

Most semiconductor alloy AxB1-x has a non-linear dependence of its band gap Eg(x) as a function of the alloy composition x, and the variation is usually described by a parabolic function Eg(x) = x•EgA + (1-x)•EgB - bg•x•(1-x), where EgA and EgB are the band gaps of A and B at their respective equilibrium lattice constants and bg is the so-called bowing parameter. The conventional band-edge distribution of bg is usually described by the equation bVBM(CBM) = ΔEVBM(CBM)/ΔEg•bg , where ΔEVBM(CBM)   and ΔEVBM(CBM) are VBM and CBM natural band offsets.

Using first-principles calculations, we investigate the unusual nonlinear behaviors of the band gaps in SnxGe1-x alloys. We show that the large bowing of the direct band gap is induced by the disordering effect. Moreover, we calculated individual contribution of the band edge states and find that the bowing of the conduction band edge is much larger than the bowing of the valence band edge, although the natural valence band offset between Ge and Sn is larger than the natural conduction band offset. The breakdown of the band-edge distribution rule is explained by the large lattice mismatch between Ge and Sn and the large deformation potential of the band edge states.