Steered Molecular Dynamics

Yu Wang and Jiping Huang

Phys. Dept., Fudan Univ., Shanghai, People’s Republic of China

Abstract

We investigate the dynamics of the detachment of single polyethylene (PE) chains from a strongly adsorbing surface in vacuum by steered molecular dynamics method. Various statistical properties, including the mean-square end-to-end distance , the mean-square radii of gyration 、, the shape factor , the torsion angle distribution, the average surface adsorption energy , the average total energy , and the average force , are analyzed. The relationship between the average force  and the pulling velocity  shows two distinctive regions: a weakly dependence region as < Å/ps and a strongly dependence region as > Å/ps.  Remarkably, the PE chain manifests force hysteresis under sequential stretching and releasing.

Keywords: Steered molecular dynamics; conformation; elasticity; adsorbed polyethylene chain