# Magneto-transport in Single Crystalline Bismuth Thin Films

Shunhao Xiao*, Dahai Wei, and Xiaofeng Jin

Surface Physics Laboratory, Fudan University, Shanghai 200433, China

Bulk Bi is a prototype semimetal. The possible existence of its semiconductor phase in thin film has attracted lots of attentions both theoretically and experimentally, yet is still a controversial issue [1-4]. In this work, the conductance and Hall coefficient of a series of single crystalline bismuth films epitaxially grown on BaF2(111) were measured as a function of film thickness and temperature, and the semimetal to semiconductor transition was clearly observed. The transport behavior in Bi film can be well explained by considering the coexistence of a metallic surface state and a semiconductor film.

[1] V. B. Sandomirskii, JETP, 25,101 (1967).

[2] C. A. Hoffman, etc. Phys. Rev. B. 48, 11431(1993), Phys. Rev. B. 51, 5535 (1995)

[3] H. T. Chu Phys. Rev. B. 51, 5532 (1995)

[4] T. Hirahara, etc. Appl. Phys. Lett. 91, 202106 (2007)