Abstract Submitted to the SNS2010

International Conference on Spectroscopies in Novel Superconductors

Shanghai, China, May 24-28, 2010

The in-plane thermal conductivity  of overdoped BaFe1.73Co0.27As2 single crystal: Evidence for nodeless multiple superconducting gaps and interband interactions

Shiyun Zhou

Department of Physics, Surface Physics Laboratory (National Key Laboratory), Laboratory of Advanced Materials, Fudan University, Shanghai 200433, People’s Republic of China

The in-plane thermal conductivity of overdoped iron-arsenide superconductor BaFe1.73Co0.27As2 (Tc = 8.1 K) single crystal was measured down to 80 mK. In zero field, the residual linear term 0/T is negligible, suggesting a nodeless superconducting gap in the ab-plane. In low magnetic field, 0/T increases sharply, very different from conventional s-wave superconductors Ba1-xKxFe2As2 and BaFe1.9Ni0.1As2 near optimal doping. It reveals an exotic superconducting gap structure in overdoped BaFe1.73Co0.27As2: the vanishing hole (β) pocket has a much larger gap than the electron (γ and δ) pockets, although the electron pockets have much larger density of states. Such an exotic gap structure is an evidence for the theory of interband superconductivity, which of great importance to understand the superconducing state in FeAs-based superconductors.