## Slide 1: A Novel Charge-trap Memory based on MoS2
State Key Laboratory of Surface Physics and Department of Physics, Fudan University,
Shanghai 200433, China.
Enze Zhang and Faxian Xiu*
Ⅰ. Introduction: Two dimensional material like graphene and molybdenum disulfide has been extensively studied recently because of their noval physical properties and promising applications in electronic devices. Here, we report on a top gated charge-trap memory composed of a molybdenum disulfide channel and a 3-dimensionl charge-trap gate stack.The fabricated memory device shows a wide memory window of more than 16V at the program/erase voltages of ±26V. Also, it displays a long retention time and highly endurance of over hundreds of cycles.
(a)
(b)
(c)
(d)
Figure 1. (a) Optical image, (b)schematic structure and(c)(d) band diagram of the charge trap memory.
Ⅱ. Structure:
Ⅲ. FET performance:
Ⅳ. Memory performance:
Figure2.(a)Id-Vd and (b)Id-Vg of the charge trap memory.
Figure 3.
(a) memory window, (b) memory window’s relation with Vg.max, (c)dynamic behavior, (d)endurance and (e)retention time of the charge trap memory.
Ⅴ. Summary :
Our charge trap memory shows a very large memory window of 16V highly endurance of more than 120 circles and a long retention time. The integration of 2-D materials with conventional charge trap gate stacks shows a great prospective in nonvolatile memory devices.
(b)
(c)
(a)
(b)
*To whom correspondence should be addressed: faxian@fudan.edu.cn
(e)
(d)
(a)