## Slide 1
Electronically phase separated nano-network in antiferromagnetic insulating LaMnO3/PrMnO3/CaMnO3 tricolor superlattice
Qiang Li1,2*, Tian Miao2,4*, Huimin Zhang2,3,7*, Weiyan Lin1, Wenhao He1,2, Yang Zhong2,3,7, Lifen Xiang2, Lina Deng2, Biying Ye2, Qian Shi2, Yinyan Zhu1,7,8, Hangwen Guo1,7,8, Wenbin Wang1,7,8, Changlin Zheng1,2, Lifeng Yin1,2,5,6,7,8, Xiaodong Zhou1,7,8†, Hongjun Xiang2,3,7† and Jian Shen1,2,5,6,7,8†
1State Key Laboratory of Surface Physics and Institute for Nanoelectronic Devices and Quantum Computing, Fudan University, Shanghai 200433, China
2Department of Physics, Fudan University, Shanghai 200433, China
3Key Laboratory of Computational Physical Sciences (Ministry of Education) and Institute of Computational Physical Sciences, Fudan University, Shanghai 200433, China
4School of Materials Science and Engineering, Xi’an Jiaotong University, Xi’an, Shanxi 710049, China
5Shanghai Research Center for Quantum Sciences, Shanghai 201315, China
6Collaborative Innovation Center of Advanced Microstructures, Nanjing 210093, China
7Shanghai Qi Zhi Institute, Shanghai 200232, China
8Zhangjiang Fudan International Innovation Center, Fudan University, Shanghai 201210, China
ANNUAL ACADEMIC CONFERENCE 2022
R-LPCMO
O-LPCMO
EPS network
SrTiO3 domain walls
MFM
sMIM
3 GHz
Sr
c
c
Ti
O
c
-10
0
10
15 deg
-15
-5
5
1T
(b)
3T
(c)
5T
(d)
0.1T
(f)
-0.2T
(g)
-0.5T
(h)
-1T
(i)
-3T
(j)
-5T
(k)
-8T
(l)
0.5T
(a)
2 m
8T
(e)
(m)
20
-20
-40
-70
0
50 mV
2 m
0T
4T
9T
(a)
(b)
(c)
(d)
EPS nano-network triggered by the structural domain formation of the underlying STO
One-to-one correspondence between ferromagnetic (AFM) to metallic (insulating) state in manganite
R-LPCMO with EPS
STO structural transition
2 m
[100]
[010]
AFM
[001]
[010]
[100]
[001]
[110]
[1-10]
0 DW
45 DW
MFM image (12K)
sMIM image (2K)
Magnetic force microscopy(MFM)
——Magnetism
Scanning Microwave Impedance Microscopy (sMIM)
——Conductivity
STEM
Background
Result
Density Functional Theory calculation
Conclusions
Jahn-Teller distortion
Compressive strain
PDOS and charge density in A-AFM state
(b)
(a)
(c)
(d)
Reference:
Miao, T. et al. Direct experimental evidence of physical origin of electronic phase separation in manganites. PNAS 117, 7090-7094 (2020).
Li, Q. et al. Electronically phase separated nano-network in antiferromagnetic insulating LaMnO3/PrMnO3/CaMnO3 tricolor superlattice. Nature Communications 13, 6593 (2022).
O-LPCMO without EPS
0°/90°——FMM state
45°/135°——EPS state
Electronic phase separation(EPS)
Ferromagnetic metallic state(FMM)
Antiferromagnetic charge-ordered insulator (AFM-COI)