姓名、电话

徐振 55664595 13774250698

报告形式：海报

标题：Single laser induced dynamic magnetization reversal mechanism of perpendicularly magnetized L10 FePt films

摘要：

Single laser pulse induced dynamic coercivity cannot be measured rigorously by the conventional time-resolved magneto-optical Kerr effect technique because the irreversible deviation of the transient magnetization is accumulated. In order to remove the accumulation effect, the alternating magnetic field is employed and synchronized with the femtosecond laser pulse. Since the sample is reset before each single laser pulse, the accumulation effect of the irreversible deviation of the transient magnetization is removed. For perpendicularly magnetized L10 FePt films, the dynamic magnetization reversal process is accomplished by the nucleation of reversed domains and the pinned domain wall motion.