Fractal plasmonic metamaterials for subwavelength imaging

Xueqin Huang*, Shiyi Xiao, and Lei Zhou

Abstract

Surface plasmon polaritons (SPPs) are elementary electromagnetic (EM) excitations bounded at metal/dielectric interfaces, and attracted considerable attention recently. For a natural material, its plasmon frequency () is fixed by the electron density, so that many SPP-based applications only work at a single frequency. Recently, people showed that Bragg scatterings can modulate the SPPs significantly, and found high optical transmissions in a silver film drilled with periodic holes [1]. However, the Bragg mechanism can not change theof a material. In 2004, Pendry et al. demonstrated that a metallic plate with periodic square holes can mimic a plasmonic metamaterial in terms of SPP properties. However, to make the idea work, one has to fill the holes with high-index materials [2], which is not easy to realize in practice, particularly at higher frequencies. Very recently, Shin et al. [3] showed that high-index insertion is not necessary if the square holes are replaced by closely packed narrow rectangle holes with cross sections. However, the generated SPPs on such structures only have transverse-magnetic (TM) polarization traveling along one direction.

We show that a metallic plate with fractal-shaped slits can be homogenitized as a plasmonic metamaterial with plasmon frequency dictated by the fractal geometry. Owing to the all-dimensional subwavelength nature of the fractal pattern, our system supports both transverse-electric and TM surface plasmons. As a result, this structure can be employed to focus light sources with all-dimensional subwavelength resolutions and enhanced field strengths. Microwave experiments reveal that the best achievable resolution is only, and FDTD simulations demonstrate that similar effects can be realized at infrared frequencies with appropriate designs.

[1] T. W. Ebbesen et. al., Nature 391, 667 (1998).

[2] J. B. Pendry, L. Martin-Moreno, F. J. Garcia-Vidal, Science 305, 847 (2004).

[3] Y. Shin, et al., Phys. Rev. Lett. 99, 147402 (2007).

*Presenting author, Email: xqhuang@fudan.edu.cn