High-resolution angle-resolved photoemission spectroscopy study of the electronic structure of EuFe2As2

Bo Zhou1, Yan Zhang1, Le-Xian Yang1, Min Xu1, Cheng He1, Fei Chen1, Jia-Feng Zhao1,Hong-Wei Ou1,

Jia Wei1, Bin-Ping Xie1, Tao Wu2, Gang Wu2, Masashi Arita3, Kenya Shimada3, Hirofumi Namatame3,

Masaki Taniguchi3, X. H. Chen2, and D. L. Feng1

1Department of Physics, Surface Physics Laboratory (National Key Laboratory), and Advanced Materials Laboratory, Fudan University, Shanghai 200433, People’s Republic of China

2Hefei National Laboratory for Physical Sciences at Microscale and Department of Physics, University of Science and Technology of China, Hefei, Anhui 230026, People’s Republic of China

3Hiroshima Synchrotron Radiation Center and Graduate School of Science, Hiroshima University, Hiroshima 739-8526, Japan

We report the high-resolution angle-resolved photoemission spectroscopy studies of electronic structure of EuFe2As2. The paramagnetic state data are found to be consistent with density-functional calculations. In the antiferromagnetic ordering state of Fe, our results show that the band splitting, folding and hybridization evolve with temperature, which cannot be explained by a simple folding picture. Detailed measurements reveal that a tiny electron Fermi pocket and a tiny hole pocket are formed near (π,π) in the (0,0)-(π,π) direction, which qualitatively agree with the results of quantum oscillations, considering kz variation of Fermi surface. Furthermore, no noticeable change within the energy resolution is observed across the antiferromagnetic transition of Eu2+ ordering, suggesting weak coupling between Eu sublattice and FeAs sublattice.

* B. Zhou et al., Phys. Rev. B 81, 155124 (2010)